X - The Neo-Babylonian Private House 2

1. Historical building name: House 2. 2. Location according to the schematic plan: the residential quarter to the East of the southern part of the Processional Way; between the reconstruction of the Ishtar of Agade Temple and the Nabu sha Hare Temple. The area was called by R. Koldewey Merkes.

3. Lay-out of the historical building: Not available.

4. Description of the present state of preservation: a complete reconstruction of a Neo-Babylonian house on the original foundations and remnants of the walls. It has rectangular shape, measuring 24,50 x 17,30 m. A/ Façades: The Northern Façade: Fig. 1 There is a very shallow buttress. Two pipes for raining water at the top. Made of contemporary baked bricks covered with the cement mortar and clay plaster overlay. Three losses of plaster. Seven huge losses of mud plaster. Loss of mortar (strip of 0,5 m width at the bottom) The Eastern Façade: Fig. 2 Characteristic “saw-toothed” wall, four pipes for raining water at the top. Destroyed plaster in the middle from the bottom to the top. The strip of 0.8 m width at the bottom – the plaster moist, cracked with losses. The contemporary baked bricks covered with deposit of dissolved salts. There are ceramic tiles between the house No 1 and the house No 2. The Southern Façade: Fig. 3 Characteristic “saw-toothed” wall, two vents, one pipe for raining water at the top. Here and there cracked plaster. In some places in the western part the plaster is coming off. The mud plaster 0,6 m high is almost totally destroyed at the ground level. The Western Façade: Fig. 4 Characteristic “saw-toothed” wall, three entrances and two vents. The plaster is in good condition. In the upper part and in the northern part, the mud (in a great percentage) is washed away from the plaster. Major losses of the plaster at the bottom and at the top. B/ Roof: There is no entrance to the roof inside. Fig. 5 C/ Interior: Northern entrance Courtyard– Floor: Fig. 6 Paved with the square ceramic tiles. In the north-western part, purposely made a circular hole, built around with two rows of the contemporary baked bricks. The well collects water through the holes at the bottom row of the bricks. There is a palm inside the well. Courtyard – The Northern Wall: Fig. 7 The minor losses of the plaster both at the bottom and at the top. Plenty of cracked plaster. Courtyard – The Eastern Wall: Fig. 8 There are some losses of the plaster at the bottom and at the top as well as at the southern part. Great percentage of washed away clay from the plaster caused by the rain water. Courtyard – The Southern Wall: Fig. 9 Partial losses of the plaster, especially in the eastern part. There are some deposits of dissolved salt places up to 0,8 m high above the floor level in the south-eastern corner. Courtyard – The Western Wall: Fig. 10 The strip up to 0,8 m high above at the floor – plaster cracked, air bubbles. The plaster outside layer is coming off. Some minor losses of the plaster at the bottom and at the top. The room located North of the courtyard – Floor: Fig. 11 The floor is paved with the square ceramic tiles, here and there sand and droppings. The room located North of the courtyard – Ceiling: Fig. 12 The reed mats are partially moist and torn. The room located North of the courtyard – The Northern Wall: Fig. 13 There are cobwebs and some minor losses of the cement plaster. The room located East of the courtyard – The Eastern Wall: Fig. 14 The thin cement plaster, visible outline of the bricks under it. There is the vent at the top in the middle of the niche. In the southern part and in the lower part – loss of the plaster, deposit of dissolved salts on the brick surface. A large loss of the plaster (1,5 x 1,8 m) in the southern part. Traces of droppings. The room located East of the courtyard – The Southern Wall: Fig. 15 The traces of water stains and droppings. Destroyed plaster in a strip up to 1,5 m high above the floor level. Major losses in the lower part. The room located East of the courtyard – The Western Wall: Fig. 16 The destroyed thin cement plaster in the southern part near at the entrance to the courtyard. The passage to the courtyard – on the southern wall S destroyed plaster up to 1,3 m high above the floor level. Four rooms located South of the courtyard – Floor: Fig. 17 Fig. 18 Made of cement tiles, a lot of droppings. The fallen off plaster is lying along the wall. Four rooms located South of the courtyard – Ceiling: Fig. 19 Fig. 20 The reed mats indicate the presence of dampness. Four rooms located South of the courtyard – Walls: Fig. 21 Fig. 22 Cobwebs, water stains, droppings. Some parts have losses of plaster (strip up to 1,5 m high above the ground level, damages noticeable especially near the floor). In several places dissolved salts crystallized in a form of efflorescence. Four rooms located West of the courtyard– Floor: Fig. 23 Fig. 24 Covered with the ceramic square tiles. Some places soiled with the dropped plaster. Four rooms located West of the courtyard – ceiling: Fig. 25 Fig. 26 Traces of dampness on the reed mats – white coating. Four rooms located West of the courtyard – The Walls: Fig. 27 Fig. 28 In some places the plaster is destroyed up to 0,8 m high above the ground level. There are crystallized dissolved salts in the places of the losses. The middle entrance - Three rooms – Floor: Fig. 29 Fig. 30 Made of ceramic tiles, they are covered with layer of mud and sand, droppings. There is a significant number of contemporary sun-dried bricks. The middle entrance – Three rooms – Ceiling: Fig. 31 Fig. 32 The wooden beams and the reed mats are moist. There is a white coating on the reed mats. The middle entrance - Three rooms – The Walls: Fig. 33 Fig. 34 There are some losses of plaster near the floor up to 0,6 m high above the floor level; the plaster is falling off and cracking. Huge deposits of dissolved salts in the places of the losses. There is a vent, and below it – traces of droppings Scratches on the plaster – Arabic and Latin inscriptions. The southern entrance - three rooms– floor: Fig. 35 Fig. 36 Paved with cement tiles, covered with the thick layer of mud. Dropped plaster near the walls. The middle entrance – Three rooms – Ceiling: Fig. 37 Fig. 38 Moist wooden beams and some traces of dampness on the reed mats. The middle entrance - Three rooms – The Walls: Fig. 39 Fig. 40 Soiled areas with droppings, cobwebs, rain water stains. The most badly destroyed plaster is in a strip up to 0,7 m high above the ground floor – major losses and detachment. The effect of efflorescence visible in the places of the losses of the plaster. Description elaborated on 18th – 19th November 2004 and photographs taken on 19th-20th November 2004 by Mirosław OLBRYŚ (Poland). The photograph no. 5 was taken by Agnieszka Dolatowska in July 2004. Translated into English by Mirosław Olbryś and Piotr Szarżanowicz on 26th November 2004. Edited by George Gogolewsky on 29th November 2004.